## Slide 1: Electro-migration Reliability Verification of Gate Level Blocks for High Performance Microprocessors in Presence of Self-Heating
Nagu Dhanwada2, Leon Sigal1, David Kadzov2
1IBM Research
2IBM Systems

## Slide 2: Motivation
EM reliability verification is a key challenge in the design of a microprocessor in the 14 nm technology.
Increasing interconnect current densities, higher current drive of FINFETs, a multi-billion transistor chip, and elevated temperatures due to local self-heating all required us to look for a robust EM verification methodology.
Since large parts of the design were implemented out of library cells, we needed to devise an efficient method of verifying each cell’s EM reliability

## Slide 3: Background
Current in the interconnect is a function of voltage, frequency, capacitance on outputs, and transition time (slew) of inputs.
The current limit of the interconnect is a function of layout (interconnect length, width and metal level), temperature and power-on-hours (POH).
Self-heating in cells depends on power and thermal resistance (RTH), the latter a function of the layout.

## Slide 4: Main Idea
Characterization of standard cells in the library for Rth, Max Slew and Max Cap.
Validation of cell instances for EM during either the block construction or sign-off phase.

## Slide 5: Characterization Phase Details -- RTH.
  Transistor models in the Physical Design Kit (PDK) provide RTH values for isolated FETs as a function of the number of fingers and FINs.
  Using this information and accounting for NFET-PFET proximity in the layout, we computed a RTH value for each library cell.
  Knowing a cell’s RTH and the power for each instance, allowed us to compute Delta T, the temperature rise due to self-heating, where DT=RTH*Power.
Notes: Example for an inverter, 1.3x NFET-PFET proximity uplift comes from TCAD modeling and test chip validation.

## Slide 6: Characterization Phase Details – Max Slew
MAX_SLEW. A set of MAX_SLEW tables at different Temp/POH points were generated for each cell.
Each table has Voltage and Frequency as independent variables. Each entry in MAX_SLEW table contains the maximum allowed slew on the input that just satisfies EM requirements.
  Larger slews create cross-over (short-circuit) currents that violate the requirements.
For simplicity, one set of MAX_SLEW tables were generated for multi-input cells. Each entry for a Voltage and Frequency combination in the table was generated through circuit simulations where the capacitance on all outputs was set to zero. Additionally, each combination was also checked to ensure IRMS and Peak currents would satisfy EM requirements by running a simulation with very fast slew of 10ps.
To determine the EM requirements failure point, either multiple simulation iterations with the input slew increasing until the failure point is observed, or several simulations at different slew points with the failure point interpolated, can be done. MAX_SLEW tables assure EM robustness in most of the interconnect of the cell, except for that of the outputs.
In the table shown, the entry for 0.6V and 0.1GHz has a maximum allowed slew of 1 ns; however, the entry at 1.2V and 8GHz is -1, indicating this design point is invalid and the IRMS, Peak, or IDC currents somewhere in the interconnect of this cell violate EM requirements for that Voltage and Frequency

## Slide 7: Characterization Phase Details – Max Cap
MAX_CAP: A set of MAX_CAP tables at different Temp/POH points were generated for each output port of every cell.
Each table could have Frequency, Voltage and Input Slew as independent variables to properly model single stage cells. Instead, we chose to limit MAX_CAP tables to Voltage and Slew only, while fixing Frequency to 25 MHz.
Values in the MAX_CAP tables are then scaled to the actual Frequency used. Each entry in the MAX_CAP table contains the maximum allowed capacitance on the output that just satisfies EM requirements.
Larger capacitances create currents that violate the requirements.
During characterization, only the interconnect associated with a specific output port is checked. When characterizing cells for MAX_CAP, the EM failure point is derived from simulations similar to those for MAX_SLEW. MAX_CAP tables ensure EM robustness in all the output interconnect of the cell.
In the table shown, the entry for 0.6V and 4 ps has a maximum capacitance of 1 pF; however, the entry for 1.2V and 2000 ps is -1, indicating this design point is invalid and the IDC currents in this output’s interconnect violate EM requirements for this Voltage and Input Slew.

## Slide 8: Main Idea – Validation Phase Details

## Slide 9: Experimental Results
Example report at the sign-off phase listing a cell instance in violation of the MAX_CAP limit, as well as violation statistics for a subset of blocks.
Left over violations were fixed manually. MAX_CAP and MAX_SLEW violations were fixed via known techniques.
High DT violations were fixed by either reducing instance power by lowering load capacitance, or increasing the instance power level.

## Slide 10: Conclusion
we used a two-step method of library cell characterization and correct-by-construction (or sign-off) validation to check EM compliance of cell-based blocks in the presence of self-heating.
This method was successfully used to verify an EM design of multi billion transistor, 5+ GHz microprocessor.