## Slide 1: Electromigration Signoff Based on IR-Drop Degradation Assessment
Electromigration Signoff Based on IR-Drop Degradation Assessment
Electromigration is the movement of metal atoms along the wire by the applied electric current.
When many atoms were moved out of the cathode region voids can be formed
Voids increase resistances of the affected metal wires.
This can lead to undesirable changes in chip operations, for example, the timing violations can be developed.
An intensity of void generation and, hence, a rate of resistance degradation can be reduced by limiting wire electric currents.
Foundries introduce special design rules – CURRENT DENSITY DESIGN RULES, which should be obeyed in all chip designs.
Valeriy Sukharev and Jun-Ho Choy - Mentor, a Siemens Business, Fremont, CA, USA
Armen Kteyan - Mentor, a Siemens Business, Yerevan, Armenia
Farid N. Najm - Department of Electrical and Computer Engineering, University of Toronto, Toronto, Canada
e-, Cu
e-, Cu
M2 test-structure
M1 test-structure
Diffusion barriers
Voids

## Slide 2: Electromigration-Induced Design Problem
With technology scaling:
The current densities in metal lines have been increasing
The electromigration (EM) lifetimes of metal lines have been decreasing
With Current Circuit-Level Reliability Assessment:
Expected development of current densities (Jmax,) needed for driving four inverter gates, according to ITRS 2011.
Current Circuit-Level Reliability Assessment:
From measured TTFs two parameters of Black’s equation: n – a current density exponent, and Ea – an activation energy are extracted
These parameters are used for calculating MTTF for other load conditions – j and T
Decompose an interconnect layout on individual segments.
Remove all segments with (jL)<(jL)crit from further consideration.
Calculate MTTF for all remaining segments.
Assume failure occurs when shortest MTTF is reached.
The expected lifetime of the overall system of interconnects is determined from the failure probability of the individual wire segments.
Material Flow is ignored
There are no diffusion barriers between segments of P/G, so atoms can freely flow from one segment to another.
Thus, there is no severe atom depletion and accumulation at each segment ends.
Voids are not expected to be formed at all segment cathode ends.
Redundancy is unaccounted for
The grid has redundancy and can survive several line failures
The series model assumption
A series model is the case where a power grid is deemed to have failed as soon as the first of its branches has failed, typically due to an open circuit. However, modern power grids use a mesh structure. As such, there are many paths for the current to flow from the flip-chip bumps to the underlying logic, a characteristic we are referred to as a redundancy. As such, it is highly pessimistic to assume that a single branch failure will always cause the whole grid to fail.
1 2 3 4 5 6
Current density in MA/cm²
Minimum gate length in nm
18 17 15 14 13 12 11 10 9 8 7
Currently used manufacturing solutions
Manufacturable EM-robust solutions are known
Manufacturable EM-robust solutions are NOT known
Required current density for driving four inverter gates
2014 2016 2018 2020 2022 Year

## Slide 3: Progress Toward Failure
t1 t2 t3
t4 t5 t6
The key feature is that a grid is deemed to have failed, not when the first line fails, but when the voltage drop at any grid node exceeds a user specification.
This leads to inaccurate EM prediction during design, sometimes optimistic and often too pessimistic
  A tree may be deemed immortal if lines are too short (Blech)
  The grid has redundancy and can survive several line failures
This calls for significant over-design. However, today, there is very little margin left for electromigration!
We find that the pessimism is very high: grids that must survive 10 years, are being designed to survive ~40 years. One might think that pessimism is not a bad strategy in VLSI. However, too much pessimism in the power grid can be a big problem. It leads to overuse of metal area, leaving little room for signal routing, which makes EM signoff extremely difficult in modern designs, thus increasing design complexity and design time.
Traditional empirical models are no longer sufficient and we need better physical models:
A. S. Oates (TSMC) ““… it is necessary to include electromigration-induced mechanical stresses in addition to current densities to accurately predict failure of circuit interconnects.” In: Interconnect reliability challenges for technology scaling: A circuit focus,” in 2016 IEEE International Interconnect Technology Conference, May 2016.

## Slide 4: EM-induced MTTF Analysis: Methodology/Tool-prototype
1-D Korhonen’s model provides EM-induced stress evolution inside single-link interconnect segment:
Applying Korhonen’s model at every segment, combined with the boundary laws, gives a fully determined system
Boundary conditions:
We discretize this in time and space and solve it to give the stress evolution at every point of interconnect tree
Effect of temperature on MTF
Accounting for the temperature distribution across the metal layers is done by employing a standard compact thermal model that represents die as array of cuboidal thermal cells with effective local thermal properties.
Voiding kinetics
For more accurate simulations, void growth model was implemented: after detecting void nucleation, the tool tracks void length
Early failure
A large void right below a via can lead to an open circuit because capping layer is non-conductive: early failures.
Using Actual Temp
Using Avg Temp
MTF~13 yrs
MTF~20 yrs

## Slide 5: Performance / Experimental Results
Power Grids |  |  |  |  | Perform.
Grid | # of nodes | # of branches | # of trees | # of current sources | CPU time
Ibmpg1* | 6K | 11K | 709 | 11K | 0.6min
Ibmpg2* | 62K | 61K | 462 | 61K | 1.2min
Ibmpg3* | 410K | 401K | 8.1K | 401K | 4.2min
Ibmpg4* | 475K | 465K | 9.6K | 465K | 6.6min
Ibmpg5* | 249K | 496K | 2K | 496K | 1.8min
Ibmpg6* | 404K | 798K | 10.2K | 798K | 14.0min
Ibmpgnew1* | 316K | 698K | 19.5K | 698K | 4.8min
Ibmpgnew2* | 718K | 698K | 19.5K | 698K | 3.6min
Power Grid1 (65nm) 14.4x12.8 mm | 13.167M | 10.708M | 2.459M | 768 | 3.5h
Power Grid2 (28nm) 4.1x6.1 mm | 15.520M | 12.448M | 2.784M | 3.150M | 6.5h
Chart: 
| ibmpg1 | ibmpg2 | ibmpg3 | ibmpg4 | ibmpg5 | ibmpg6 | ibmpgnew1 | ibmpgnew2
Blacks Model Mesh MTF (yrs) | 11.7375 | 2.9385 | 3.9114 | 2.0091 | 2.9015 | 2 | 3.1964 | 4.6344
Extended Korhonen's model Mesh MTF (yrs) | 6.1 | 6.6298 | 6.09 | 8.77 | 5.86 | 8.0828 | 12.13 | 5.3
Monte-Carlo approach allows to study the random distribution of diffusivities in wires, and to estimate the voiding probability for branches of the simulated interconnect trees.
Each Monte-Carlo experiment provides a list of all voided branches. The lists of voided branches, generated by all performed MC iterations, allow to get voiding statistics (i.e. the voiding probability for each branch). This information is visualized in Calibre RVE.
For 20 branches voiding probability is in the range ~36 – 41%; this is 6.73% of total number of branches in M3 layer for which voiding was detected (297)
e-
High voiding probability (P=90.625%) in the highlighted branch is due to high current inflow.

## Slide 6: CONCLUSIONS: Physics-Based EM Assessment is DEVELOPED
Given:
  Power Grid (DC, RC, or RLC netlist)
  Tolerance for grid node voltage fluctuations (Vth)
  Effective DC for block currents
Find:
  Evolution of the voltage drop variations on the grid caused by EM induced segment resistance growth
Features:
  Source currents/T0 voltage drop/Resistors are from any Power Tool (Mentor’s BlueWafe).
Results:
  Power Grid Mean Time to Failure (MTF)
  There are many improvements in performance, power, time-to-market and design cost that become possible if the developed physics-based EM checking is used.
Forward EM assessment problem is solved!
Removing the over conservative foundry-based current design rules can help to extend a technology-node life-time!
Experimental proof
C. Gan, C. Thompson, et. Al, J. Appl. Phys. 94, 1222, 2003.
Reference structure.
Redundant structure.
B. Quattara, L. Doyen, et al., Microelectronics Reliability, 54 (2014), 1702.
Redundant structure is characterized by two abrupt jumps of resistance, while the reference structure demonstrated just one coincident with the first jump in redundant. Same MTTF are obtained for both structures although the total current in the redundant structure is two times higher.
B. Li, et al. in IEEE IRPS Proceedings, South San Francisco, CA, 2018, pp. 4F3.1 - 5.
Redundancy doesn’t only provide the alternative current paths, but also allows the electric current to redistribute when the EM induced void causes a local resistance increase.